**Top Natur Glaze**

**Directions for Use**

**Preparation**

* Contour resin, then finish with coarse silicone point or carbide bur.
* Steam or ultrasound clean surface, dry, then remove leftover residue with mild detergent or ethanol on applicator. Direct application of ethanol can cause micro-cracks.
* Surface must be rough, as **Top Natur Glaze** will not adhere to polished surfaces.

**Application**

* Direct application with brush.
* Do not air blow air dry.
* Transparent.
* Comes in ½ oz. and 1 oz. containers.

**Recommended Indications for Coating**

* Indirect composite surfaces, interproximal areas and fissures.
* Denture base surfaces.
* Provisional materials.

Consistency can be adjusted by adding **Top Airstain/natur glaze Thinner.**

**Precautions**

* Avoid high-stress bearing areas like occlusal surfaces.